Centrifuge Model Testing of Liquefaction Mitigation via Microbially-Induced Calcite Precipitation

Dexter Harris Jr.

University of California, Davis – Center for Geotechnical Modeling

ABSTRACT

A new, innovative soil strengthening geochemical process, microbially-induced calcite precipitation (MICP) has been studied more in recent years. The advantage to using this technique as opposed to other soil strengthening techniques is that it is more environmentally friendly, which bodes well for the soil attempted to be strengthened and the surrounding areas. This paper presents data from three models, two of which were treated with MICP. Cementation was measured using shear wave velocity and calcite content measurements. Because the method of creating the model and conducting the MICP test on the second tested model was altered, the results were slightly different. However, an increase in shear wave velocity or calcite content measurement still correlated to a higher level of cementation.

INTRODUCTION

For many years, scientists and engineers have been attempting to master an understanding of how soil works and if the structure of various soils can be improved. There has been extensive research done on this and ground improvement techniques have been invented and implemented but there is a concern over the balance between the improvement of the soil and the long-term health of the soil as a result of the ground improvement techniques. More recently, biomediated geochemical processes, which consist of a geochemical reaction regulated by subsurface microbiology (DeJong, 2013), have been gaining traction in terms of becoming primary ground improvement techniques. Examples of these processes include gas generation, biofilm formation and biopolymer generation.

One of the more intriguing processes is microbially-induced calcite precipitation (MICP). This process uses a natural biologically mediated method to create cementation in situ and improve the mechanical soil properties (DeJong, 2006). MICP uses urea hydrolysis as the chemical reaction to induce calcite precipitation (Fujita, 2008). The purpose of MICP is to strengthen soil to reduce the effects of liquefaction. In the past, geotechnical centrifuge tests have performed to attempt to understand how MICP works but more tests have to be conducted in order to further understand the behavior of MICP when subjected to repeated shaking events.

MATERIALS AND METHODOLOGY

Model Construction

Three Ottawa sand models were build in a plexiglass container and saturated with deionized water. The first model was made in order to calculate the flow rate of our deionized water and cementation solution for the second model. This section will cover the second and third models made as they were used to collect data.

The second model consisted of six layers of material: gravel, mesh, Monterey sand, F65 Ottawa sand, mesh, and gravel. The bottom layer of gravel and the Monterey sand were both approximately 1 cm thick, the Ottawa sand was 10 cm thick (placed in the model in 2 cm lifts), and the top layer of gravel was approximately 5 cm thick. Mesh was placed between the bottom layer of gravel and the Monterey sand in order to prevent the sand from seeping into the gravel, which would affect the solutions’ ability to travel throughout the model.

There were seven bender element pairs placed in the model, placed at four vertical depths and two horizontal distances at each vertical depth. The spacing between the two bender elements of each pair ranged from 5.8-8.5 cm. One bender was set as the transmitter and one as the receiver; the transmitter sent out a signal to the receiver and that signal is what was monitored in order to collect data. Figure 1 and table 1 show the plan view of the model.

The third model differed from the second model slightly. There were no mesh layers; based on the second model’s data it was hypothesized that the mesh potentially impeded the solutions from uniformly travelling throughout the model. The bottom layers of gravel and Monterey sand were combined; the total height of the layer was still a combined 2 cm. The Ottawa sand was still placed in the model in 2 cm lifts; however, the total height of the Ottawa sand was 8.7 cm. The top layer of gravel was increased from 5 cm to 7.6 cm. Bender element pairs were only placed in three vertical depths but they were placed at two horizontal distances at each vertical depth, similar to the second model.  Figure 9 and table 3 show the plan view of the model.

Model Treatment

The second model was first saturated with deionized water for a little over 24 hours, followed by two pore volumes of S. pasturii in a saline solution. The model then sat for 12 hours in order for the bacteria to settle within the model. Each treatment thereafter consisted of deionized water, CaCl2, and urea. The treatment was pumped into the model after shear wave velocities were collected, which occurred approximately six hours after the conclusion of the previous treatment. Nine treatments were performed with ten total shear wave velocity measurements being taken, including the initial measurement.

The third model was saturated with deionized water for approximately 28 hours, followed by four pore volumes of S. pasteurii in a saline solution. The inoculation process consisted of three stages: pumping of the S. pasteurii from the bottom up at 0.17 L/min, gently pouring the S. pasteurii over the top of the model while running the pump in reverse, and a repeat of the first step. The first step lasted for 2 hrs and 35 min, the second lasted for 1 hr and 20 min, and the third for 2 hrs.

The treatments consisted of pumping two pore volumes of treatment solution from the bottom up into the model. The solution for this test also has yeast extract and sodium acetate along with the other materials used in the solution for the second model. As opposed to every six hours, treatments were conducted every 12 hours for this model; the solution was pumped bottom-up into the model at a rate of 0.34 L/min. Shear wave velocity measurements were collected before each measurement.

DATA

For both models, shear wave velocity measurements and calcite content measurements were collected. A larger shear wave measurement corresponds to more cementation occurring in that region, as does a larger calcite content. For each region measured, one shear wave velocity measurement was taken at each region for both the second and third model. For the second model, calcite content measurements were taken in 10 g amounts and 3 measurements were taken and averaged at each region; for the third model, the amount measured varied, and two or three measurements were taken and averaged at the discretion of the data collector. Figures 2-8 and table 2 show the data collected for the second model, while table 4 shows the data collected for the third model.

RESULTS

For the second model, there was a very distinct difference in the cementation that occurred on the transmitter side of the model as opposed to the receiver model. This lack of uniformity could have been the result of multiple factors but it was concluded that the mesh used magnified the lack of uniformity, hence the absence of it in the third model.

The shear wave velocity measurements for the third model were considerably higher than expected, which made the calcite content measurements that much more intriguing to get, since calcite content and shear wave velocity measurements should coincide with each other. The bottom lift of the Ottawa sand was the most cemented, as expected, but pouring the S. pasteurii over the model led to the surface of the Ottawa sand being the second most cemented layer.

CONCLUSION

Microbially-induced calcite content is an environmentally friendly soil strengthening geochemical process that uses bacteria to create cementation. In order to test the effectiveness of MICP, models have to be created and pumped with microbes and treatment solutions. During the duration of this portion of the research, two models were created and tested. The results of each of the tests varied but the third model created was closer to giving a result of uniformity after testing, which is a very important component in trying to implement this technique in a real world scenario. More models will be made and tested until results come back satisfactory enough to conduct a centrifuge test using the adjusted model.

ACKNOWLEDGEMENTS

I would like to thank NHERI and the NSF for accepting me into this program and providing the funding necessary for me to conduct this research. I would to thank the University of California, Davis for hosting me and allowing me to use their materials and laboratories. I would like to thank my faculty mentor, Jason DeJong and my graduate mentors, Kathleen Darby and Gabby Hernandez for their taking the time out to guide me through this process. Their continuous support and constant sharing of knowledge made this experience worthwhile.

REFERENCES

DeJong, J. T., Fritzges, M. B. & Nu ̈sslein, K. (2006). Microbial induced cementation to control sand response to undrained shear. J. Geotech. Geoenviron. Engng 132, No. 11, 1381– 1392.

DeJong, J. T. et al. (2013). Geotechnique 63, No. 4, 287–301

Fujita, Y., Taylor, J. L., Gresham, T. T., Delwiche, M., Colwell, F., McLing, T. L., Petzke, L. M. & Smith, R. W. (2008). Stimula- tion of microbial urea hydrolysis in groundwater to enhance calcite precipitation. Environ. Sci. Technol. 42, No. 8, 3025– 3032.

FIGURES AND TABLES

Figure 1. Plan view of model.  Bender elements are depicted by rectangles, injection ports are depicted by circles.

| Transmitter | Receiver | Spacing (cm) | Depth | Location | Corresponding Figure |
| --- | --- | --- | --- | --- | --- |
| B2 | B9 | 6.5 | Lift 1 | A1 | Figure 8 |
| B3 | B5 | 8.5 | Lift 2 | A1 | Figure 7 |
| B6 | B11 | 7.3 | Lift 2 | A2 | Figure 4 |
| B10 | B12 | 5.8 | Lift 3 | A1 | Figure 6 |
| B13 | B14 | 7 | Lift 3 | A2 | Figure 3 |
| B17 | B18 | 7.5 | Lift 4 | A1 | Figure 5 |
| B21 | B22 | 7.5 | Lift 4 | A2 | Figure 2 |

Table 1. Bender locations and spacing.  *Note: Lift 4 is shallow, Lift 1 is deep

| Location | A-1 | Center | A-2 |
| --- | --- | --- | --- |
|  | Calcite content (%) |  |  |
| Lift 4 | 0.11 | 0.32 | 0.85 |
| Lift 3 | 0.12 | 0.80 | 1.20 |
| Lift 2 | 0.31 | 1.18 | 1.39 |
| Lift 1 | 0.75 | 0.98 | -- |
|  | Final Vs (m/s) |  |  |
| Lift 4 | 84.5 | -- | 366 |
| Lift 3 | 77 | -- | 464 |
| Lift 2 | 248 | -- | 557 |
| Lift 1 | 481 | -- | -- |

Table 2. Calcite contents and shear wave velocity measurements after 9 treatments *Note: Lift 4 is shallow, Lift 1 is deep

Figure 2. Shear wave velocity for B21B22 (shallowest bender in array 2)

Figure 3. Shear wave velocity for B13B14 (mid-depth bender in array 2)

Figure 4. Shear wave velocity for B6B11 (deepest bender in array 2)

Figure 5. Shear wave velocity for B17B18 (shallowest bender in array 1) Unreliable

Figure 6. Shear wave velocity for B10B12 (upper mid-depth bender in array 1) Unreliable

Figure 7. Shear wave velocity for B3B5 (lower mid-depth bender in array 1)

Figure 8. Shear wave velocity for B2B9 (deepest bender in array 1)

Figure 9. Plan (top) and side (bottom) view of the model.  Each lift is approximately 2 cm thick.

| Transmitter | Receiver | Spacing -PS (cm) | Spacing -ES (cm) | Lift No. | Depth (cm) | Array No. |
| --- | --- | --- | --- | --- | --- | --- |
| B6 | B11 | 7.4 | 7.9 | 2 | 13.7 | A1 |
| B3 | B5 | 6.9 | 6.6 | 3 | 11.0 | A1 |
| B15 | B16 | 6.25 | 6.4 | 4 | 9.1 | A1 |
| B2 | B9 | 7.4 | 7.4 | 2 | 13.7 | A2 |
| B13 | B14 | 7.5 | 7.4 | 3 | 11.0 | A2 |
| B21 | B22 | 7.4 | 7.6 | 4 | 9.1 | A2 |

Table 3. Bender locations and spacing.  *Note: Lift 4 is shallow, Lift 2 is deep

| Pea Gravel |  |  |  |
| --- | --- | --- | --- |
|  | A1 | Center | A2 |
| L5 | 4.3% | 2.5% | 4.4% |
| L4 | 1.2% (1357 m/s) | 0.9% | 1.7% (1535 m/s) |
| L3 | 2.1% (729 m/s) | 0.2% | 3% (1053 m/s) |
| L2 | 8.3% (2083 m/s) | 1.3% | 5.5% (1758 m/s) |
| L1 |  |  |  |
| Pea Gravel/Monterey Matrix |  |  |  |

Table 4. Average calcite contents and shear wave velocity measurements after 6 treatments and a DI flush in side view (top). Average calcite content for lift 3 in plan view (bottom).